## Slide 1: CH-4: Imperfections in Solids
So far we have seen perfect crystals: X-ray diffraction and Bragg’s law
Imperfections or defects are covered in ch-4.
Defects in crystals make them interesting
2 major types of defects: Chemical – Impurities or Alloying elements Atomic arrangement- Structure
Real materials are not perfect
Good Chemical Imperfections: dopants & alloying element
Atomic arrangements: missing atom, extra atom, differently oriented unit cells, etc…

## Slide 2: Why STUDY Imperfections in Solids?
Many of the important properties of materials are due to the presence of imperfections.
Pure metals experience significant alterations when alloyed: Sterling silver: 92.5% Ag & 7.5% Cu. Cartridge brass: 70% Cu & 30% Zn.
Impurities play important roles in semiconductors.
Steel (composition ) and (making)
Atomic defects are responsible for reducing gas pollutant emissions in automobiles:
Molecules of pollutant gases become attached to surface defects of crystalline metallic materials ((Ce0.5Zr0.5)O2) in the catalytic converter. While attached to these sites, chemical reactions convert them into other non- or less-polluting substances.

## Slide 3: Catalyst: (Ce0.5Zr0.5)O2
High-resolution transmission electron micrograph of single crystal (Ce0.5Zr0.5)O2,which is used in Catalytic Converters.
Catalyst is a substance that speeds up the rate of a chemical reaction without participating in the reaction itself.
Catalyst adsorbs on its surface gas pollutants (CO and NOX) and molecules of unburned hydrocarbons, which are converted to CO2 and H2O.
Active sites on catalysts are normally surface defects
Schematic representation of surface defects that are potential adsorption sites for catalysts.

## Slide 4: http://auto.howstuffworks.com/catalytic-converter2.htm
In the catalytic converter, there are two different types of catalyst at work, a reduction catalyst and an oxidation catalyst. Both types consist of a ceramic structure coated with a metal catalyst, usually platinum, rhodium and/or palladium. The idea is to create a structure that exposes the maximum surface area of catalyst to the exhaust stream, while also minimizing the amount of catalyst required, as the materials are extremely expensive.
The catalyst used in a catalytic converter is a combination of platinum (Pt), palladium (Pd), and rhodium (Rh). These metals coat a ceramic honeycomb (or ceramic beads) contained within a metal casing that is attached to the exhaust pipe. The catalytic converter’s honeycomb structure provides the maximum surface area on which reactions can take place while using the least amount of catalyst. - See more at: http://www.explorecuriocity.org/Content.aspx?contentid=1779#sthash.ygSRJfFB.dpuf

## Slide 5: Types of Imperfections
• Vacancy atoms
• Interstitial atoms
• Substitutional atoms
Point defects
• Dislocations
Line defects
• Grain Boundaries
Area defects

## Slide 6: Point Defects in Metals
• Vacancies:
-vacant atomic sites in a structure.
• Self-Interstitials:
-"extra" atoms positioned between atomic sites.
Vacancy
distortion
of planes
self-
interstitial
distortion
of planes

## Slide 7: Equilibrium Concentration: Point Defects
æ
Boltzmann's constant
(1.38 x 10
-23
J/atom-K)
(8.62
x
10
-5
eV/atom-K)
N
v
N
=
exp

Q
v
k
T
è
ç
ö
ø

No. of defects
No. of potential
defect sites
Activation energy
Temperature
Each lattice site
is a potential
vacancy site
• Equilibrium concentration varies with temperature!

## Slide 8: Measuring Activation Energy
• We can get Qv from
an experiment.
æ
ç
N
v
N
=
exp
-
Q
v
k
T
è
ç
ö
ø

• Measure this...
N
v
N
T
exponential
dependence!
defect concentration
• Replot it...
1/
T
N
N
v
ln
-
Q
v
/k
slope

## Slide 9: Estimating Vacancy Concentration
• Find the equil. # of vacancies in 1 m3 of Cu at 1000C.
• Given:
A
Cu
= 63.5 g/mol
r
= 8.4 g
/
cm
3
Q
v
= 0.9 eV/atom
N
A
= 6.02 x 1023
atoms/mol
For 1 m3
, N =
N
A
A
Cu
r
x
x
1 m3
= 8.0 x 1028 sites
= 2.7 x 10-4
8.62 x 10-5
eV/atom-K
0.9 eV/atom
1273 K
ç
N
v
N
=
exp
-
Q
v
k
T
æ
è
ç
ö
ø

• Answer:
N
v
=
(2.7 x 10-4)(8.0 x 1028) sites = 2.2 x 1025 vacancies

## Slide 10
4.1 Calculate the fraction of atom sites that are vacant for lead at its melting temperature of 327°C (600 K). Assume an energy for vacancy formation of 0.55 eV/atom.
4.3 Calculate the activation energy for vacancy formation in aluminum, given that the equilibrium number of vacancies at 500C (773 K) is 7.57  1023 m-3. The atomic weight and density (at 500C) for aluminum are, respectively, 26.98 g/mol and 2.62 g/cm3.

## Slide 11: Impurities in Solids
A pure metal consisting of only one type of atom just isn’t possible. Even with sophisticated techniques, it is difficult to refine metals to a purity in excess of 99.9999%.
Very few metals are used in the pure or nearly pure state: 1. Electronic wires- 99.99% purity Cu; Very high electrical conductivity.
2. 99.99% purity Al (super-pure Al) is used for decorative purposes-- Very bright metallic surface finish.
Most engineering metals are combined with other metals or nonmetals to provide increased strength, higher corrosion resistance, etc.
Cartridge brass: 70% Cu & 30% Zn.
Sterling silver: 92.5% Ag & 7.5% Cu.
Inconel 718, Ni-base super-alloy, used for jet engine parts, has 10 elements.

## Slide 12: Solid Solutions
Simplest type of alloy is that of solid solution.
Two types: 1. Substitution Solid Solution
2. Interstitial Solid Solution.

## Slide 13: Conditions for Solid Solubility
Conditions for substitutional solid solution (S.S.)
W. Hume – Rothery rule
  1. r (atomic radius) < 15%
  2. Proximity in periodic table
    i.e., similar electronegativities
  3. Same crystal structure for pure metals
  4. Same Valency
An example of a substitutional solid solution is found for copper and nickel. These
two elements are completely soluble in one another at all proportions.
The atomic radii for copper and nickel are 0.128 and 0.125 nm, respectively; both have the FCC crystal structure; their electronegativities are 1.9 and 1.8 and their valences match.

## Slide 14: Application of Hume–Rothery rules – Solid Solutions
Element Atomic Crystal Electro- Valence Radius Structure nega- (nm) tivity
Cu 0.1278 FCC 1.9 +2 C 0.071 H 0.046 O 0.060 Ag 0.1445 FCC 1.9 +1 Al 0.1431 FCC 1.5 +3 Co 0.1253 HCP 1.8 +2 Cr 0.1249 BCC 1.6 +3 Fe 0.1241 BCC 1.8 +2 Ni 0.1246 FCC 1.8 +2 Pd 0.1376 FCC 2.2 +2 Zn 0.1332 HCP 1.6 +2 Pt 0.1387 FCC 2.2 +2
4.4: Which of these elements would you expect to form the following with copper: (a) A substitutional solid solution having complete solubility
(b) A substitutional solid solution of incomplete solubility
(c) An interstitial solid solution

## Slide 15: Interstitial Solid Solutions

## Slide 16: Computation of Radius of BCC Octahedral Interstitial Site
Compute the radius r of an impurity atom that just fits into a BCC octahedral site in terms of the atomic radius R of the host atom (without introducing lattice strains).

## Slide 17: Computation of Radius of FCC Octahedral Interstitial Site
Compute the radius r of an impurity atom that just fits into a FCC octahedral site in terms of the atomic radius R of the host atom (without introducing lattice strains).

## Slide 18: Computation of Radius of BCC Tetrahedral Interstitial Site
Compute the radius r of an impurity atom that just fits into a BCC tetrahedral interstitial site in terms of the atomic radius R of the host atom (without introducing lattice strains).