## Slide 1: Chapter 2: Atomic Structure & Interatomic Bonding
ISSUES TO ADDRESS...
• What promotes bonding?
• What types of bonds are there?
• What properties are inferred from bonding?

## Slide 2
http://web.mit.edu/newsoffice/2008/adhesive-0218.html
http://robotics.eecs.berkeley.edu/~ronf/Gecko/index.html
Gecko’s toe pads
Extremely large number of microscopically small hairs
gecko-inspired bandage (ultrastrong synthetic adhesives):
for use in surgical procedures as a replacement for sutures and staples to close wounds and incisions. This material retains its adhesive nature in wet environments, is biodegradable, and does not release toxic substances as it dissolves during the healing process.
A gecko can support its body mass with a single toe! The secret to this remarkable ability is the presence of an extremely large number of microscopically small hairs on each of their toe
pads. When these hairs come in contact with a surface, weak forces of attraction (i.e., van der Waals forces) are established between hair molecules and molecules on the surface. The fact that these hairs are so small and so numerous explains why the gecko grips surfaces so tightly. To release its grip, the gecko simply curls up its toes and peels the hairs away from the surface.

## Slide 3: Atomic Structure (Freshman Chem.)
atom – electrons – 9.11 x 10-31 kg protons neutrons
atomic number = # of protons in nucleus of atom = # of electrons of neutral species
A [=] atomic mass unit = amu = 1/12 mass of 12C Atomic wt = wt of 6.022 x 1023 molecules or atoms 1 amu/atom = 1g/mol
C 12.011 H 1.008 etc.
} 1.67 x 10-27 kg

## Slide 4: Isotopes
2.2 Chromium has four naturally-occurring isotopes: 4.34% of 50Cr, with an atomic weight of 49.9460 amu, 83.79% of 52Cr, with an atomic weight of 51.9405 amu, 9.50% of 53Cr, with an atomic weight of 52.9407 amu, and 2.37% of 54Cr, with an atomic weight of 53.9389 amu. On the basis of these data, confirm that the average atomic weight of Cr is 51.9963 amu.

## Slide 5: Electric Charge
Atomic Particle
Charge
Mass
Electron
–1.6  10-19 C
9.11  10-31 Kg
Proton
+1.6  10-19 C
1.673  10-27 Kg
Neutron
0
1.675  10-27 Kg
Atomic Model
The coulomb unit is derived from the SI unit ampere for electric current i. Current is the rate dq/dt at which charge moves through a region.

## Slide 6: Atomic Structure
Valence electrons determine all of the following properties
    Chemical
    Electrical
    Thermal
    Optical

## Slide 7: Electronic Structure
Electrons have wavelike and particulate properties.
  This means that electrons are in orbitals defined by a probability.
  Each orbital at discrete energy level is determined by quantum numbers. Quantum # Designation
  n = principal (energy level-shell) K, L, M, N, O (1, 2, 3, etc.)
  l = subsidiary (orbitals) s, p, d, f (0, 1, 2, 3,…, n -1)
  ml = magnetic 1, 3, 5, 7 (-l to +l)
  ms = spin ½, -½

## Slide 8: Electron Energy States
1s
2s
2p
K-shell n = 1
L-shell n = 2
3s
3p
M-shell n = 3
3d
4s
4p
4d
Energy
N-shell n = 4
• have discrete energy states
• tend to occupy lowest available energy state.
Electrons...
Adapted from Fig. 2.4, Callister & Rethwisch 8e.

## Slide 9: SURVEY OF ELEMENTS
• Most elements: Electron configuration not stable.
Electron configuration
(stable)
...
...
1s
2
2s
2
2p
6
3s
2
3p
6
(stable)
...
1s
2
2s
2
2p
6
3s
2
3p
6
3d
10
4s
2
4p
6
(stable)
Atomic #
18
...
36
Element
1s
1
1
Hydrogen
1s
2
2
Helium
1s
2
2s
1
3
Lithium
1s
2
2s
2
4
Beryllium
1s
2
2s
2
2p
1
5
Boron
1s
2
2s
2
2p
2
6
Carbon
...
1s
2
2s
2
2p
6
(stable)
10
Neon
1s
2
2s
2
2p
6
3s
1
11
Sodium
1s
2
2s
2
2p
6
3s
2
12
Magnesium
1s
2
2s
2
2p
6
3s
2
3p
1
13
Aluminum
...
Argon
...
Krypton
Adapted from Table 2.2, Callister & Rethwisch 8e.

## Slide 10: Electron Configurations
Valence electrons – those in unfilled shells
Filled shells more stable
Valence electrons are most available for bonding and tend to control the chemical properties
  example: C (atomic number = 6)
    1s2 2s2 2p2
valence electrons

## Slide 11: Electronic Configurations
ex: Fe - atomic # =
26
valence
electrons
Adapted from Fig. 2.4, Callister & Rethwisch 8e.
1s
2s
2p
K-shell n = 1
L-shell n = 2
3s
3p
M-shell n = 3
3d
4s
4p
4d
Energy
N-shell n = 4
1s2 2s2 2p6 3s2 3p6
3d 6 4s2

## Slide 12: The Periodic Table
• Columns: Similar Valence Structure
Adapted from Fig. 2.6, Callister & Rethwisch 8e.
Electropositive elements:
Readily give up electrons
to become + ions.
Electronegative elements:
Readily acquire electrons
to become - ions.
give up 1e-
give up 2e-
give up 3e-
inert gases
accept 1e-
accept 2e-
O
Se
Te
Po
At
I
Br
He
Ne
Ar
Kr
Xe
Rn
F
Cl
S
Li
Be
H
Na
Mg
Ba
Cs
Ra
Fr
Ca
K
Sc
Sr
Rb
Y

## Slide 13: Electronegativity
• Ranges from 0.7 to 4.0,
Smaller electronegativity
Larger electronegativity
• Large values: tendency to acquire electrons.
Adapted from Fig. 2.7, Callister & Rethwisch 8e. (Fig. 2.7 is adapted from Linus Pauling, The Nature of the Chemical Bond, 3rd edition, Copyright 1939 and 1940, 3rd edition. Copyright 1960 by Cornell University.

## Slide 14: Ionic bond – metal + nonmetal
donates accepts electrons electrons
Dissimilar electronegativities
ex: MgO Mg 1s2 2s2 2p6 3s2 O 1s2 2s2 2p4
[Ne] 3s2
Mg2+ 1s2 2s2 2p6 O2- 1s2 2s2 2p6
[Ne] [Ne]

## Slide 15: Ionic Bonding
• Occurs between + and - ions.
• Requires electron transfer.
• Large difference in electronegativity required.
• Example: NaCl
Na (metal)
unstable
Cl (nonmetal)
unstable
electron
+
-
Coulombic
Attraction
Na (cation)
stable
Cl (anion)
stable

## Slide 16: Bonding Forces and Energies
The origin of an attractive force FA depends on the particular type of bonding that exists between the two atoms.
Repulsive forces arise from interactions between the negatively charged electron clouds for the two atoms and are important only at small values of r as the outer electron shells of the two atoms begin to overlap.
2.13 Calculate the force of attraction between a K+ and an O2- ion the centers of which are separated by a distance of 1.5 nm.

## Slide 17: Ionic Bonding
Energy – minimum energy most stable
  Energy balance of attractive and repulsive terms
Attractive energy EA
Net energy EN
Repulsive energy ER
Interatomic separation r
r
A
n
r
B
EN = EA + ER =
+
-
Adapted from Fig. 2.8(b), Callister & Rethwisch 8e.

## Slide 18: Problem 2.14
The net potential energy between two adjacent ions, EN, may be represented by the sum of Equations 2.8 and 2.9; that is,
Calculate the bonding energy E0 in terms of the parameters A, B, and n using the following procedure:
1. Differentiate EN with respect to r, and then set the resulting expression equal to zero, since the curve of EN versus r is a minimum at E0.
2. Solve for r in terms of A, B, and n, which yields r0, the equilibrium inter-ionic spacing.
3. Determine the expression for E0 by substitution of r0 into Equation 2.11.