## Slide 1: Chap 19: Thermal Properties
Thermostat
Rail lines buckled due to unanticipated scorching heat wave occurred in Melbourne, Australia.

## Slide 2: Chapter 19: Thermal Properties
ISSUES TO ADDRESS...
• How do materials respond to the application of heat?
• How do we define and measure...
-- heat capacity?
-- thermal expansion?
-- thermal conductivity?
-- thermal shock resistance?
• How do the thermal properties of ceramics, metals, and polymers differ?

## Slide 3: Heat Capacity
• Quantitatively: The energy required to produce a unit rise in temperature for one mole of a material.
heat capacity
(J/mol-K)
energy input (J/mol)
temperature change (K)
• Two ways to measure heat capacity: Cp : Heat capacity at constant pressure.
Cv : Heat capacity at constant volume.
Solids: Cp = Cv
• Heat capacity has units of
The ability of a material to absorb heat
Gases: Cp > Cv

## Slide 4: Dependence of Heat Capacity on Temperature
• Heat capacity...
-- increases with temperature
-- for solids it reaches a limiting value of 3R
• From atomic perspective:
-- Energy is stored as atomic vibrations.
-- As temperature increases, the average energy of atomic vibrations increases.
Adapted from Fig. 19.2, Callister & Rethwisch 8e.
R = gas constant
3R
= 8.31 J/mol-K
Cv = constant
Debye temperature
(usually less than T
room
)
T (K)
q
D
0
0
Cv

## Slide 5: Atomic Vibrations
Atomic vibrations are in the form of lattice waves or phonons. A phonon is analogous to the photon in electromagnetic radiation.

## Slide 6: Specific Heat Capacity
The heat Q that must be supplied or removed to change the temperature of a substance of mass m by an amount DT is,
where c is the specific heat capacity of the substance.
Unit for Specific Heat Capacity:
SI: J/(kg · C°)
cgs: cal/(g. C°)

## Slide 7: Specific Heat: Comparison
increasing cp
Selected values from Table 19.1, Callister & Rethwisch 8e.
• Polymers
Polypropylene
Polyethylene
Polystyrene
Teflon
cp (J/kg-K)
at room T
• Ceramics
Magnesia (MgO)
Alumina (Al2O3)
Glass
• Metals
Aluminum
Steel
Tungsten
Gold
1925
1850
1170
1050
900
486
138
128
cp (specific heat): (J/kg-K)
Material
940
775
840
Cp (heat capacity): (J/mol-K)

## Slide 9
At low temperatures the relationship between Cv and the absolute temperature is
….. Eq. 19.2
3R
0
T (K)
Cv

## Slide 10
19.1 Estimate the energy required to raise the temperature of 2 kg (4.42 lbm) of the following materials from 20 to 100°C (68 to 212°F): aluminum, steel, soda–lime glass, and high-density polyethylene.

## Slide 11: Thermal Expansion
Materials change size when temperature is changed
linear coefficient of
thermal expansion (1/K or 1/ºC)
Tinitial
Tfinal
 initial
 final
Tfinal > Tinitial

## Slide 12: Atomic Perspective: Thermal Expansion
Adapted from Fig. 19.3, Callister & Rethwisch 8e.
Asymmetric curve:
-- increase temperature, -- increase in interatomic separation -- thermal expansion
Symmetric curve:
-- increase temperature, -- no increase in interatomic separation -- no thermal expansion

## Slide 13: Coefficient of Thermal Expansion: Comparison
• Q: Why does a
generally decrease
with increasing
bond energy?
Polypropylene
145-180
Polyethylene
106-198
Polystyrene
90-150
Teflon
126-216
• Polymers
• Ceramics
Magnesia (MgO)
13.5
Alumina (Al2O3)
7.6
Soda-lime glass
9
Silica (cryst. SiO2)
0.4
• Metals
Aluminum
23.6
Steel
12
Tungsten
4.5
Gold
14.2
a (10-6/C) at room T
Material
Polymers have larger  values because of weak secondary bonds
increasing 
A: The greater the bond energy, the deeper and more narrow this potential energy trough.

## Slide 14: Thermal Expansion: Example
Ex: A copper wire 15 m long is cooled from 40 to -9ºC. How much change in length will it experience?
Answer: For Cu
rearranging Equation 19.3b

## Slide 15: Invar and Other Low-Expansion Alloys
Super Invar: 63 wt% Fe, 32 wt% Ni, and 5 wt% Co.
Kovar: 54 wt% Fe, 29 wt% Ni, and 17 wt% Co. Its thermal expansion is similar to that of Pyrex glass.
Invar means invariable length. Charles-Edouard Guillaume won the 1920 Nobel prize in physics for discovering Invar: 64 wt% Fe-36 wt% Ni.
As a specimen of Invar is heated, within its Curie temperature (~2300C), its tendency to expand is countered by a contraction phenomenon that is associated with its ferromagnetic properties (magnetostriction).
http://www.youtube.com/watch?v=ZoGBjGKlLcU