## Slide 1: Chapter 3: The Structure of Crystalline Solids
ISSUES TO ADDRESS...
• How do atoms assemble into solid structures?
• How does the density of a material depend on
its structure?
• When do material properties vary with the
sample orientation?

## Slide 2
X-ray diffraction photograph for a single crystal of magnesium.
Photograph of a single crystal of magnesium that was cleaved (or split) along a (0001) plane—the flat surface is a (0001) plane. Also, the direction perpendicular to this plane is a [0001] direction.
Mag Wheel—a lightweight automobile wheel made of magnesium.

## Slide 3
After studying this chapter you should be able to do the following:
Describe the difference in atomic/molecular structure between crystalline and noncrystalline materials.
Draw unit cells for face-centered cubic, body-centered cubic, and hexagonal close-packed crystal structures.
Derive the relationships between unit cell edge length and atomic radius for face-centered cubic and body-centered cubic crystal structures.
Compute the densities for metals having face-centered cubic and body-centered cubic crystal structures given their unit cell dimensions.
Given three direction index integers, sketch the direction corresponding to these indices within a unit cell.
Specify the Miller indices for a plane that has been drawn within a unit cell.
Describe how face-centered cubic and hexagonal close-packed crystal structures may be generated by the stacking of close-packed planes of atoms.
Distinguish between single crystals and polycrystalline materials.
Define isotropy and anisotropy with respect to material properties.

## Slide 4: Energy and Packing
• Non dense, random packing
• Dense, ordered packing
Dense, ordered packed structures tend to have
lower energies.
Energy
r
typical neighbor
bond length
typical neighbor
bond energy
Energy
r
typical neighbor
bond length
typical neighbor
bond energy

## Slide 5: Materials and Packing
• atoms pack in periodic, 3D arrays
Crystalline materials...
-metals
-many ceramics
-some polymers
• atoms have no periodic packing
Noncrystalline materials...
-complex structures
-rapid cooling
crystalline SiO2
noncrystalline SiO2
"Amorphous" = Noncrystalline
Adapted from Fig. 3.23(b),
Callister & Rethwisch 8e.
Adapted from Fig. 3.23(a),
Callister & Rethwisch 8e.
Si
Oxygen
• typical of:
• occurs for:

## Slide 6: Metallic Crystal Structures
How can we stack metal atoms to minimize empty space?
2-dimensions
vs.
Now stack these 2-D layers to make 3-D structures

## Slide 7: Metallic Crystal Structures
• Tend to be densely packed.
• Reasons for dense packing:
- Typically, only one element is present, so all atomic
radii are the same.
- Metallic bonding is not directional.
- Nearest neighbor distances tend to be small in
order to lower bond energy.
- Electron cloud shields cores from each other
• Have the simplest crystal structures.
We will examine three such structures...

## Slide 8: Simple Cubic Structure (SC)
• Rare due to low packing density (only Po has this structure)
• Close-packed directions are cube edges.
• Coordination # = 6
(# nearest neighbors)
Click once on image to start animation
(Courtesy P.M. Anderson)

## Slide 9: Atomic Packing Factor (APF):SC
• APF for a simple cubic structure = 0.52
APF =
APF =
Volume of atoms in unit cell*
Volume of unit cell
*assume hard spheres
Adapted from Fig. 3.24,
Callister & Rethwisch 8e.
close-packed directions
a
R=0.5a
contains 8 x 1/8 =
1
atom/unit cell

## Slide 10: Body Centered Cubic Structure (BCC)
• Coordination # = 8
Adapted from Fig. 3.2,
Callister & Rethwisch 8e.
• Atoms touch each other along cube diagonals.
--Note: All atoms are identical; the center atom is shaded
differently only for ease of viewing.
ex: Cr, W, Fe (), Tantalum, Molybdenum
2 atoms/unit cell: 1 center + 8 corners x 1/8
Click once on image to start animation
(Courtesy P.M. Anderson)

## Slide 11: Atomic Packing Factor: BCC
a
• APF for a body-centered cubic structure = 0.68
a
R
Adapted from
Fig. 3.2(a), Callister & Rethwisch 8e.
a
2
a
3
APF =

## Slide 12: Face Centered Cubic Structure (FCC)
• Coordination # = 12
Adapted from Fig. 3.1, Callister & Rethwisch 8e.
• Atoms touch each other along face diagonals.
--Note: All atoms are identical; the face-centered atoms are shaded
differently only for ease of viewing.
ex: Al, Cu, Au, Pb, Ni, Pt, Ag
4 atoms/unit cell: 6 face x 1/2 + 8 corners x 1/8
Click once on image to start animation
(Courtesy P.M. Anderson)

## Slide 13: Atomic Packing Factor: FCC
• APF for a face-centered cubic structure = 0.74
maximum achievable APF
a
2 a
Adapted from
Fig. 3.1(a),
Callister & Rethwisch 8e.

## Slide 14
A sites
B
B
B
B
B
B
B
C
sites
C
C
C
A
B
B
sites
• ABCABC... Stacking Sequence
• 2D Projection
• FCC Unit Cell
FCC Stacking Sequence
B
B
B
B
B
B
B
B
sites
C
C
C
A
C
C
C
A
A
B
C

## Slide 15: Hexagonal Close-Packed Structure (HCP)
• Coordination # = 12
• ABAB... Stacking Sequence
• APF = 0.74
• 3D Projection
• 2D Projection
Adapted from Fig. 3.3(a),
Callister & Rethwisch 8e.
6 atoms/unit cell
ex: Cd, Mg, Ti, Zn
• c/a = 1.633 (for ideal)
c
a
A sites
B
sites
A sites
Bottom layer
Middle layer
Top
layer

## Slide 16
For the HCP crystal structure, show that the ideal c/a ratio is 1.633.

## Slide 17
1. Show that the base area of the unit cell for HCP is given by, 6√3R2.
2. Show that the atomic packing factor for HCP is 0.74.