## Slide 1: Theoretical Density, r
where n = number of atoms/unit cell
A = atomic weight
VC = Volume of unit cell = a3 for cubic
NA = Avogadro’s number
= 6.022 x 1023 atoms/mol
Density =  =
VC NA
n A
 =
Cell
Unit
of
Volume
Total
Cell
Unit
in
Atoms
of
Mass
Chapter 3: The Structure of Crystalline Solids

## Slide 2: Theoretical Density, r
Ex: Cr (BCC)
A = 52.00 g/mol
R = 0.125 nm
n = 2 atoms/unit cell
theoretical
a = 4R/ 3 = 0.2887 nm
ractual
a
R
 =
a3
52.00
2
atoms
unit cell
mol
g
unit cell
volume
atoms
mol
6.022 x 1023
= 7.18 g/cm3
= 7.19 g/cm3
Adapted from
Fig. 3.2(a), Callister & Rethwisch 8e.

## Slide 3: Densities of Material Classes
r
metals
>
r
ceramics
>
r
polymers
Why?
Data from Table B.1, Callister & Rethwisch, 8e.
r
(g/cm )
3
Graphite/
Ceramics/
Semicond
Metals/
Alloys
Composites/
fibers
Polymers
1
2
2
0
30
B
ased on data in Table B1, Callister
*GFRE, CFRE, & AFRE are Glass,
Carbon, & Aramid Fiber-Reinforced
Epoxy composites (values based on
60% volume fraction of aligned fibers
in an epoxy matrix).
10
3
4
5
0.3
0.4
0.5
Magnesium
Aluminum
Steels
Titanium
Cu,Ni
Tin, Zinc
Silver, Mo
Tantalum
Gold, W
Platinum
G
raphite
Silicon
Glass
-
soda
Concrete
Si nitride
Diamond
Al oxide
Zirconia
H
DPE, PS
PP, LDPE
PC
PTFE
PET
PVC
Silicone
Wood
AFRE
*
CFRE
*
GFRE*
Glass fibers
Carbon
fibers
A
ramid fibers
Metals have...
• close-packing
(metallic bonding)
• often large atomic masses
Ceramics have...
• less dense packing
• often lighter elements
Polymers have...
• low packing density
(often amorphous)
• lighter elements (C,H,O)
Composites have...
• intermediate values
In general

## Slide 4: Crystals as Building Blocks
• Some engineering applications require single crystals:
• Properties of crystalline materials
often related to crystal structure.
(Courtesy P.M. Anderson)
-- Ex: Quartz fractures more easily along some crystal planes than others.
-- diamond single
crystals for abrasives
-- turbine blades
Fig. 8.33(c), Callister & Rethwisch 8e. (Fig. 8.33(c) courtesy of Pratt and Whitney).
(Courtesy Martin Deakins,
GE Superabrasives, Worthington, OH. Used with permission.)

## Slide 5: Polycrystals
• Most engineering materials are polycrystals.
• Nb-Hf-W plate with an electron beam weld.
• Each "grain" is a single crystal.
• If grains are randomly oriented,
overall component properties are not directional.
• Grain sizes typically range from 1 nm to 2 cm
(i.e., from a few to millions of atomic layers).
Adapted from Fig. K, color inset pages of Callister 5e.
(Fig. K is courtesy of Paul E. Danielson, Teledyne Wah Chang Albany)
1 mm
Isotropic
Anisotropic

## Slide 6: Single vs Polycrystals
• Single Crystals
-Properties vary with
direction: anisotropic.
-Example: the modulus
of elasticity (E) in BCC iron:
Data from Table 3.3, Callister & Rethwisch 8e. (Source of data is R.W. Hertzberg, Deformation and Fracture Mechanics of Engineering Materials, 3rd ed., John Wiley and Sons, 1989.)
• Polycrystals
-Properties may/may not
vary with direction.
-If grains are randomly
oriented: isotropic.
(Epoly iron = 210 GPa)
-If grains are textured,
anisotropic.
200 mm
Adapted from Fig. 4.14(b), Callister & Rethwisch 8e.
(Fig. 4.14(b) is courtesy of L.C. Smith and C. Brady, the National Bureau of Standards, Washington, DC [now the National Institute of Standards and Technology, Gaithersburg, MD].)
E (diagonal) = 273 GPa
E (edge) = 125 GPa

## Slide 7: Polymorphism
Two or more distinct crystal structures for the same material.
Allotropy-when found in elemental solids. titanium
, -Ti
  carbon
diamond, graphite
BCC
FCC
BCC
1538ºC
1394ºC
912ºC
-Fe
-Fe
-Fe
liquid
iron system
Allotropy of iron

## Slide 8: Tin (Its Allotropic Transformation)
White (or beta) tin, having a body-centered tetragonal crystal structure at room temperature, transforms, at 13.2°C (55.8°F), to gray (or alpha) tin, which has a crystal structure similar to diamond.
The rate at which this change takes place is extremely slow; however, the lower the temperature (below 13.2°C) the faster the rate.
This transformation results in: Increase in volume (27 %), and, a decrease in density (from 7.30 g/cm3 to 5.77 g/cm3). Consequently, this volume expansion results in the disintegration of the white tin metal into a coarse powder of the gray allotrope. This produced some rather dramatic results in 1850 in Russia. The winter that year was particularly cold, and record low temperatures persisted for extended periods of time. The uniforms of some Russian soldiers had tin buttons, many of which crumbled because of these extreme cold conditions, as did also many of the tin church organ pipes. This problem came to be known as the “tin disease.”

## Slide 9
3.7 Iron has a BCC crystal structure, an atomic radius of 0.124 nm, and an atomic weight of 55.85 g/mol. Compute and compare its theoretical density with the experimental value found inside the front cover.
3.8 Calculate the radius of an iridium atom, given that Ir has an FCC crystal structure, a density of 22.4 g/cm3, and an atomic weight of 192.2 g/mol.